## Slide 1: Semi-finished materials
Finger-jointed panels
Scantlings for windows and doors
Semi-finished door elements
Worktops

## Slide 2: Finger-jointed panels
Acacia
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 3: Finger-jointed panels
Walnut
Quality: Rustic
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 4: Finger-jointed panels
Walnut
Quality: Rustic
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 5: Finger-jointed panels
Ash
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 6: Finger-jointed panels
Oak
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 7: Finger-jointed panels
Oak
Quality: BB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 8: Finger-jointed panels
Chestnut
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 9: Finger-jointed panels
Quality: BB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.
Chestnut

## Slide 10: Finger-jointed panels
Beech
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 11: Finger-jointed panels
Beech
Quality: BB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 12: Finger-jointed panels
Coniferous
Quality: AB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 13: Finger-jointed panels
Coniferous
Quality: BB
Thickness: 14-200mm
Width: 35-1300mm
Width of lamella: 20mm-40mm
Length: 6m
Humidity: 10% ±1.5%.
Glue: Kleibert D3, D4
May vary according customer wishes.

## Slide 14: Scantlings for windows and doors
Sizes: mm 48x95 - 120 mm 63x75 - 86 - 95 - 120 mm 66x75 - 86 - 95 - 120 mm 72x75 - 86 - 95 - 120
Specification: DKD Gluing: UNI EN 204 D4
Humidity: 10 - 12%
On request it is possible to offer different size for minimum quantity ordered.

## Slide 15: Semi-finished Door Elements
Door size (with frame) - 2200 mm, X900 mm
Board size - 2100 mm, X800 mm, X45 mm
Frame size - 70 mm, X900 mm, X2200 mm - 2 pcs, 70 mm, X90 mm, X900 mm - pcs
Lamellar width in the board: form 120 mm up to 160 mm.
The size and wood type varies according customer wishes.
We produce semi-finished elements for doors. This elements meet Euro Standards for doors. The final customer can use them for producing doors according to their own design

## Slide 16: Worktops
We offer prime quality Acacia, Walnut, Chestnut, Coniferous, Beech, Ash, Oak solid wood worktops.
Sizes depend on customer request.